TEJAGALA is a metallic roofing tile made in galvanized steel G60, coated with a polyester paint finish applied in their superior face.

It can be used in house constructions as in commercial ones; the recommended slope is of 25% (minimum 15%).

The panels of metallic roofing tiles are settle in the roofs imitating the appearance of the classic clay roofing tiles and offer many advantages on the traditional tile.

Among his main advantages it emphasizes his easy installation in relation to the traditional ones.

Advantages

- Light Ceiling System

- Does not require waterproofing (asphalt)

- Fast and Easy Installation

- Great Durability

- 1.00 mts. coverage

Composition

Metal base is structural steel degree B (resistance 37.000 psi flow) with galvanized covering G60 (approx 15 microns in each side, or 0,60 square oz./ft. between both faces), each side with a painted layer of epoxy primer base of 5 microns and finish coats of low brightness polyester terracotta color of 15 microns.

The standard of the complete material is ASTM A755 (pre-painted or enameled) on material base ASTM A653 SS Degree 37, or its analog that is ASTM A446 B Degree.

Profile Characteristics